Moving Solid Metallic Targets for Pion Production in the Muon Collider / Neutrino Factory Project

# H.G. Kirk and P. Thieberger

## BNL

FIGURES

A full version of the paper was published as MUC-NOTE-TARGET-234

Fig. 1

Fig. 2    Three-dimensional view of energy deposition MARS data for a 3 mm rms radius 16TP beam on a 7.5 mm radius iron target.

Table 1.   Maximum energy density deposited by a 16TP, 24 GeV beam in an iron target.

| Beam width [rms mm] | .5 | 1 | 1.5 | 2 | 2.5 | 3 | 3.5 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Target radius [mm] | 1.25 | 2.5 | 3.75 | 5 | 6.25 | 7.5 | 8.75 |
| Maximum energy density [J/g] | 305 | 105 | 55.6 | 36.0 | 26.5 | 22.1 | 16.5 |

Table 2.	Mechanical an thermal characteristics of the materials

|  | Density | Linear Exp. Coeff. | Young Modulus | Bulk Modu-lus | Poisson Ratio | Specific Heat @ constant pressure | Thermal Conducti-vity | Yield Stren-gth | Fatigue Endu- rance Limit |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Symbol |  |  | Y | B |  | cp |  |  | -l |
| Unit | g/cm3 | 10-6 / 0K | G Pa | G Pa |  | J/(g 0K) | W/(m 0K) | M Pa | M Pa |
| Iron | 7.87 | 12.5 | 205 | 171 | 0.30 | 0.478 | 80 | 170 | ~85 |
| Inconel 718 | 8.19 | 13.1 | 200 | 158 | 0.29 | 0.435 | 11.2 | 1034 | 586 |
| VascoMax C-350 | 8.08 | 15.0 | 200 | 167 | 0.30 | 0.450 | 25.2 | 2242 | 758 |
| Super Invar | 8.15 | 0.63 | 144 | 88.9 | 0.23 | 0.515 | 10.5 | 276 | ~138 |

Table 3.  Typical Chemical Compositions (%).

| Element | C | Al | Si | S | Ti | Cr | Mn | Fe | Co | Ni | Cu | Nb | Mo |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Atomic Number | 6 | 13 | 14 | 16 | 22 | 24 | 25 | 26 | 27 | 28 | 29 | 41 | 42 |
| Inconel 718 |  | 0.5 |  |  | 1 | 19 |  | 19 |  | 52.5 |  | 5 | 3 |
| Vasco Max C-350 | .02 | 0.1 | .05 | .005 | 1.4 |  | .05 | 63 | 12 | 18.5 |  |  | 4.8 |
| Super Invar | .05 | .07 | .09 | .01 |  | .03 | .4 | 62 | 5.4 | 31.8 | .08 |  |  |

Fig. 3

Fig. 4

Fig. 5

Fig. 6

Fig. 7

Fig 8

Fig. 9

Fig. 10

Table 4	1 MW-option results for a 7.5 mm radius target

|  | Iron | Inconel 718 | Vascomax C- 350 | Super Invar |
| --- | --- | --- | --- | --- |
| Maximum Stress/ Yield Stress | 1.7 | 0.27 | 0.16 | 0.025 |
| Maximum Stress/ Fatigue Limit | 3.3 | 0.48 | 0.47 | 0.050 |
| Available Energy/ Yield Energy | 10.9 | 0.28 | 0.09 | 0.004 |
| Available Energy/ Fatigue Energy | 43.6 | 0.87 | 0.81 | 0.014 |

Table 5   4 MW-option results for a 7.5 mm radius target

|  | Iron | Inconel 718 | Vascomax C-350 | Super Invar |
| --- | --- | --- | --- | --- |
| Maximum Stress/ Yield Stress | 3.4 | 0.54 | 0.32 | 0.05 |
| Maximum Stress/ Fatigue Limit | 6.7 | 0.95 | 0.94 | 0.10 |
| Available Energy/ Yield Energy | 24.2 | 0.61 | 0.21 | 0.008 |
| Available Energy/ Fatigue Energy | 96.8 | 1.93 | 1.79 | 0.03 |

Fig. 11    Linear expansion as a function of temperature for Invar and Supper Invar alloys.

Fig 12a							Fig. 12b

Comparison of a doubly Gaussian beam profile (a) with an ideal flat profile (b) containing the same number of particles.

Fig. 13  Octupole-lens generated beam profile compared to a Gaussian profile with the octupole turned off.

Fig. 14 	Schematic examples of metallic chain links showing rather compact designs with large metal to gap volume rtatios.

Fig.15	Schematic example of a chain with long links that would allow the beam to be coaxial with the target.

1 MW OPTION

15 pulses per second

66.7 kJ per pulse

17.3 TP per pulse

4 MW OPTION

30 pulses per second											133 kJ per pulse

34.7 TP per pulse

Fig. 16	Proton beam pulse sequences for the proposed 1 MW and 4 MW options.

Fig. 17

Fig. 18

Fig. 19

Table 6.    Examples of target velocities and lengths according to assumptions explained in the text.

|  | Velocity (continuous motion) | Minimum length (continuous motion) | Average Velocity (intermittent motion) | Minimum length (intermittent motion) |
| --- | --- | --- | --- | --- |
|  | m/s | m | m/s | m |
| Super Invar - 1 MW Option | 7.5 | 175 |  |  |
| Vascomax C-350 - 1 MW Option | 0.85 | 16.8 | 1.0 | 18 |
| Super Invar - 4 MW Option | 12.0 | 274 |  |  |
| Vascomax C-350 - 4 MW Option | 3.0 | 34 |  |  |

Fig. 20   Axial magnetic field calculated for the 20T solenoid arrangement described in the Feasibility Study1).

Fig. 21  Breaking forces per unit target length due to Eddy currents in a 1.5 cm diameter Vascomax C-target

Fig. 22  Magnetic forces on a 1.5 cm diameter Vascomax C-350 target placed in the field shown in fig. 20.

Fig. 23  Tension as a function of position for a 1.5 cm diameter Vascomax C-350 target placed in the field

Fig. 23  Tension as a function of position for a 1.5 cm diameter Vascomax C-350 target placed in the field shown in fig.20.  In this example, an external tension is applied to achieve a minimum tension of 1 MPa.

### Fig. 24

Fig 25

Fig. 26	Invar linear expansion coefficient as a function of temperature and magnetic field 19).

Fig. 27	Low temperature data20)  from Fig. 26  combined with known expansion coefficients at higher temperatures.

Table 8.    Comparison of  advantages and disadvantages the three alloys considered in this paper.

| MATERIAL | ADVANTAGES | DISADVANTAGES |
| --- | --- | --- |
| Super Invar | Largest margin for thermal shock tolerance. Absence of large magnetic forces. | Narrow temperature range and low heat conductivity leading to the need for long chains or cables. The largest uncertainty regarding deleterious effects of radiation damage. |
| Vascomax C-350 | Largest tensile strength. Good heat conductivity allowing the use of relatively short chains or cables. | The material is ferromagnetic and will be subject to large magnetic forces |
| Inconel 718 | Good fatigue endurance limit similar to Vascomax C-350. Absence of large magnetic forces. | Poor heat conductivity (similar to Super Invar) requiring long chains of cables, but not as long as for Super Invar since the temperature range is not as small. |