## Slide 1: A Dipole (without) Grain Oriented Steel

## Slide 2: Overview
Suggestion for a new dipole design
Materials
Simulation results
  achievable fields
  field quality
Power loss

## Slide 3: Grain Oriented Steel
Chosen to minimize magnetization losses
  low coercivity
  high saturation field
  (in direction of grains)
Challenges
  measuring material properties
  1D material – not very forgiving in terms of geometrical errors / material inhomogeneities
  change of material properties over time / radiation exposure
  Simulations – convergence problems
Proposal: use different materials
  FeCo (Hiperco 50A)
  6.5% silicon steel (JFE SuperCore)

## Slide 4: BH Curves
Isotropic
FeCo: saturates at higher B
6.5SiFe: developed for f>50Hz
Limits: 1.1/2.1T
(GO Steel: 1.75T)
FeCo
6.5SiFe
GO Fe

## Slide 5: New Dipole Design
Combine both to benefit from respective advantages
  Design yoke so that field around 1.1-1.2T
  Center yoke: FeCo
Geometry: Don Summers EI yoke (‘first magnet’)
Opera 3D
Looked at tapered and non-tapered designs
6.5Si Steel
FeCo

## Slide 6: Geometry
22 mm
110 mm
100 mm

## Slide 7: Magnetization

## Slide 8: Peak Field
From D. Summers: Fast Ramping 750 GeV Muon Synchrotron Dipoles
d

## Slide 9: Field Quality
Evaluate vertical magnetic field on centre plane (y=0)
  from -18 to 18 mm
Fit polynom to field:
Plot polynomial coefficients as function of peak magnetic field in centre
45 mm

## Slide 10: Forbidden Multipoles

## Slide 11: Sextupole

## Slide 12: Sextupole

## Slide 13: Decapole

## Slide 14: JFE Super Core (0.1 mm sheet)
about 10W/kg

## Slide 15: Hiperco 50A
About 20W/lb (44W/kg)

## Slide 16: Test Magnet
FeCo (1 m long magnet)
  average field 1.7T
  mass: 45 kg
  power loss: 2kW/m
6.5SiFe
  average field: 1T
  mass: 235 kg
  power loss: 2.35 kW/m
Assumes 400 Hz

## Slide 17: Things to do
Epstein frame test
  JFE will provide samples for free (cut to size)
  Hiperco 50A: identified supplier and company for cutting/annealing, waiting for quotation
If successful: test magnet, geometry close to Don’s 2nd magnet (later on: more life size model?)
Magnet design for RCS ring?

## Slide 18: Summary
FeCo + 6.5SiFe seems to be good combination
  higher field than GO steel
  better field quality?
Conceptual design of test magnet
Material tests