## Slide 1: Dipole for Fast Ramping Synchrotron

## Slide 2: Geometry
Required good field region: 62x10 mm2
Magnet aperture: 100x13 mm2
Magnet dimension:
> 500x500 mm2
FeCo
6.5%SiFe

## Slide 3: Magnetization
1 T
2 T

## Slide 4: Maximum Field
2T?

## Slide 5: Epstein Frame Test
FeCo
  enough material purchased for 9 test strips (24 planned)
6.5SiFe
  100 strips shipped (thanks to Mr. Ninomiya at JFE)
Epstein frame test at Fermilab
  thanks to Robert W Riley and John Zweibohmer

## Slide 6: 6.5 Si Steel
Measurements
  C-direction
  L-direction
  L/C direction

## Slide 7: Results 6.5% Si Steel

## Slide 8: Results 6.5% Si Steel

## Slide 9: Results 6.5% Si Steel

## Slide 10: Results 6.5% Si Steel

## Slide 11: Results 6.5% Si Steel

## Slide 12: FeCo - Hiperco
Purchased from Ed Fagan
  Hiperco 50 (A)
Cut to size on site
Annealed at IFW in Dresden, Germany
  871 deg C, 2h in vacuum

## Slide 13: FeCo – Hiperco 50A

## Slide 14: FeCo – Hiperco 50A

## Slide 15: FeCo – Comparison GO Steel

## Slide 16: Fe Co Results
about 0.1T short
reason is unknown
  wrong material
  bad batch
  not enough material
  wrong annealing
Vacuumschmelze GmbH & Co. KG
  Hanau, Germany

## Slide 17: Vacoflux 48

## Slide 18: Summary
6.5% Si steel
  confirmed values from datasheet
  almost isotropic
  good match of hysteresis loop
  losses?
FeCo
  discrepancy between datasheet and measurement
  Vacuumschmelze