## Slide 1: Explo Test and YBaCuO Jc Fit

## Slide 2: Explo Test
Aim: understand mechanical properties of HTS/Stainless composite
HTS tape co-wound with steel tape
  no epoxy
  unravel?
  friction?
F
F

## Slide 3: Explo Test
Calculations: little pre-stress should actually suffice
  needs practical verification
Test samples wound
  arrived in Oxford
  prepped for test

## Slide 4: Geometry
Zylon
HTS
Glass
4 mm

## Slide 5: Stress

## Slide 6: Winding

## Slide 7: Explo Test
Harwood Engineering high pressure rig
  up to 8 kbar
  He gas
Allows (in principle) to determine orthotropic material properties
  also at 77K
  Y.K Huang: Exploding pressure vessel test on zylon/epoxy composite. http://dx.doi.org/10.1016/S1359-8368(01)00065-8

## Slide 8: explo vessel

## Slide 9: Introduction
HTS Quench
  current in stainless tape
Interesting:
  Propagation
  Temperature
Simulation
  10 cm long stainless tape (100 um thick)
  heating: 1 mm length
  1 s, 500A
I
Quench HTS tape?

## Slide 10: Basis
Function for Jc of YBaCuO
Drew W Hazelton (SuperPower): Recent Developments in 2G HTS Coil Technology, Applied Superconductivity Conference, August 2010, Washington.
(Vito Lombardo: An Ic(B,Θ) parameterization for YBaCuO CC Tapes. FERMILAB-TM-2461-TD. )

## Slide 11: General Methodology
Universal relationship between Jc and B
  if normalized to Jc0(T) and Hirr(T)
  for different directions B//c and B//(a,b)
Angular dependence
  added later on with separate expression

## Slide 12: Jc0(T)

## Slide 13: Normal State Phase Diagram
Hirr = 120 / 900 T

## Slide 14: Universal H//c Curve

## Slide 15: Universal H//(a,b) Curve

## Slide 16: B // c Fit

## Slide 17: Average Curve, Comparison
B (T)
Jc/Jc(77K, 0T)

## Slide 18: J // c Axis
B (T)
Jc/Jc(77K, 0T)

## Slide 19: J // (a,b) Axis
B (T)
Jc/Jc(77K, 0T)

## Slide 20: Angular Dependence

## Slide 21: Angular Dependence
Presently implemented as linear function

## Slide 22: Summary
Explo test: ongoing
Function for Jc of YBaCuO
Implemented as MEX/C code
  C part can be extracted
Also: Tc function
  uses iterative method to determine Tc